## Slide 1: 2024_10_21
Dispersion at 1064nm&1550nm
Radius = 1500um
2% Unanneal/Long anneal
2x2um
For Photogalvanic, we want normal dispersion at 1064nm to avoid FWM competing power with SHG
THOX 15um thick
2x2um,2%,Air Clad

## Slide 2: 2% Unanneal, @1550nm Without fitting refractive index before simulation
Arrow means
E-field direction
The measured refractive index has fluctuations that cause the zigzag
These are two fundamental modes

## Slide 3: 2% Unanneal, @1550nm Sellmeier fitting refractive index before simulation
Zigzag disappeared after you apply Sellmeier fitting

## Slide 4: 2% Long Anneal, @1064nm Without fitting

## Slide 5: 2024_10_23
Cross Section 4x12 um
Wavelength 460, 532, 780, 1060, 1550 nm
Core Material: 2% Long anneal
Radius: Whatever captures 1B Q
Subject: Bending Q
THOX 500um thick
4x12,2%,Air Clad

## Slide 6: 1550nm

## Slide 7: 1064nm

## Slide 8: 965nm

## Slide 9: 780nm

## Slide 10: 685nm
At lower radius, Comsol is more easily to find mode that is a coexistence between the core and the cladding
The blue are very faint eigenmode of the THOX

## Slide 11: 532nm
These contains the reflection(because my PML does not perfectly absorb), also the eigenmode in THOX. I believe this is mostly eigenmode in THOX, because if it is from reflection, you should see interference pattern

## Slide 12: An example of reflection:

## Slide 13
Cross Section 4x12 um
Wavelength 460, 532, 780, 1060, 1550 nm
Core Material: 2% Long anneal
Radius: 1500um
Subject: Light Distribution Plot & effective mode area
2024_10_26

## Slide 14: E-field to the right Linear

## Slide 15
E-field to the right Log

## Slide 16: E-field Upward Linear

## Slide 17: E-field Upward Log

## Slide 18: Compare: @532nm, E-Right , Linear 2x2um(r=1000um) vs. 4x12um(r=1500um)

## Slide 19: Compare: @532nm, E-Right , Log 2x2um(r=1000um) vs. 4x12um(r=1500um)

## Slide 20: Compare: @532nm, E-Up, Linear 2x2um(r=1000um) vs. 4x12um(r=1500um)

## Slide 21: Compare: @532nm, E-Up, Log 2x2um(r=1000um) vs. 4x12um(r=1500um)

## Slide 22
2% Long Anneal
30 x 2um
@1550nm
OR1: R=3300um
OR1.5: R=2800um(6um width)
OR2: R=2250um
OR3: R=1600um
OR4: R=1050um
OR1
OR1.5
OR3
OR2
OR4
E up: Q = 0.283M
E right: Q = 2.12M

## Slide 23
2% Long Anneal
30 x 2um
@1550nm
OR1: R=3300um
OR2: R=2250um
OR3: R=1600um
OR4: R=1050um
OR1
OR2
OR3
OR4
Aeff=21.446663810347093 um^2
Aeff = 19.439836253579607 um^2

## Slide 24: 780nm 3x2 clad and non clad r=1000um
No Cladding, 780,
E right: Simulation Fluctuates a lot at the order of 10^20 Q. The bending Q should be very high
E up: B
Yes Cladding, 780,
E right: Still very high ~10^19
E up:

## Slide 25: Cladding Device, 780, up and right have almost identical mode area so I only show one of them

## Slide 26: Air Cladding, Up and Right E-field have slightly different mode distribution

## Slide 27: 2024_10_29
3x2 um, 780nm, air clad dispersion
2x2um, 532nm, air clad, dispersion, r=1000um

## Slide 28: 3x2 um, 780nm, air clad dispersion

## Slide 29: 2x2um, 532nm, air clad, dispersion, r=1000um

## Slide 30
Radius V.s. momentum
Width v.s. momentum
2x12um, R=1500um
ICP-PECVD cladding
2% long anneal
2024_11_3

## Slide 31: Steps
Get the FSR
Based on the coupling Q, calculate the target kappa
Based on the target kappa, tune the geometry for covalent bond formation

## Slide 32: Get the FSR
21.19171390008956 right
21.187508667145355 up

## Slide 33: Based on Coupling Q
Lower width, stronger momentum
Larger radius, stronger momentum(might be incorrect)

## Slide 34: Momentum and width
0.002211083304213684
1.15069203e-07
Thus, try:
Gap = 3.2um, 2x2um

## Slide 35: Momentum and Gap Size

## Slide 36: Test FUck
Problem
Under sqrt is negative
Beta21 = 2*delta_beta
Problem
When momentum is not conserved, I still find some mode, but are they coupled?
I will get an imaginary beta21, what does it mean?
Bad configuration choice
Gap = 3.2um
2x2 um
帮!

## Slide 37: Test Fuck 2
Gap = 3.37um
2x2 um
Warren Jin’s Paper about SiN
The energy profile tendency(from left to right is 1060,1064,1068).
Not the same as the paper(but I think it is normal)
帮!
Also I noticed that including or excluding PLM, the energy profile and beta are not the same
帮!

## Slide 38: Based on Test Fuck2, get the couple Q
Loss per round trip
FSR=21.19171390008956Ghz for E-right
My simulation tells me:
Beta_21 = 0.2455595259210124
delta_beta = 0.013914358123656712

## Slide 39: Third Try
Gap =4um
1.9um width

## Slide 40: Gap=4um
Very hard to match momentum, skip gap =4
1.882um --- beta21
Change width, delta beta

## Slide 41: Gap = 3.6um, still sensitive, but ok

## Slide 42
Δβ is 0.005386158311011968
|β_21| is 0.18904083071175182
Δβ / |β_21| = 0.028492036829994394

## Slide 43: Gap=4.5um

## Slide 44: Is beta 21 sensitive to waveguide width +-1nm?

## Slide 45
Difficulty: find beta21 that is small
Find momentum conservation(width, gap)

## Slide 46: 11/12 Spherical Resonators
10um
1064
Infinitely high bending Q

## Slide 47: Hunting for anomalous dispersion
532, 780,1064
2um thick(except for 1550n, that’s 4um)
Diameter = 2mm/3mm
Fundamental modes(Need to test higher modes as well)
Could be air or silica cladding

## Slide 48: 532 air clad r=1500um no fitting, 2%

## Slide 49: 532 air clad r=1500um fitting, 2%

## Slide 50: Radius = 1000um, 2um height, 1um width

## Slide 51: 2024/12/09
Sphere
2% as core
Air Clad

## Slide 52: 980

## Slide 53: 2015/1/25
Best: z=8um
Best: z=8um.
2x10um PECVD Clad.
Laser Diode is modelled as elliptical gaussian
Divergence angle: x = 22deg, y=8deg